## Slide 1: Data and Models of Solid State Structures
https://github.com/rsc-solid-data/data_diffn_crystals

## Slide 2: Structure: Foundation of materials “design”
Solid state structure underpins function in materials, from conductivity to colour.
Representations of solid-state structure are models, not direct observations.
Accurate, truly representative structural models are vital
   Valid structure-property relationships
Structure
Properties
Function and application
S. A. Kulkarni et al., J. Mater. Chem. A, 2014, 2, 9221.
Notes: S. A. Kulkarni, T. Baikie, P. P. Boix, N. Yantara, N. Mathews and S. Mhaisalkar, Band-gap tuning of lead halide perovskites using a sequential deposition process, J. Mater. Chem. A, 2014, 2, 9221–9225.

## Slide 3: Models are everywhere
Observation
Final model
Approximation, prediction
Model
Input
Output
Assumptions

## Slide 4: Models are everywhere
Model
Input
Output
Assumptions
Real crystal
Crystal structure Approximation of true atomistic arrangement (another model)
Ionic model
Hard spheres, known radii, electrostatic interactions
Crystalline solid
Regular repeat defined by periodic lattice

## Slide 5: Models are everywhere
Model
Input
Output
Assumptions
Bragg’s law
Intensities
Structure factors
Thermal effects…
e.g.
Data reliability
(sample, measurement, processing…)
Long-range, perfectly ordered structure
Time-averaged “static” structure represents dynamics adequately
Crystal structure
(another model)

## Slide 6: Models are everywhere
Model
Output
Input
Assumptions
Bragg’s law
Intensities
Structure factors
Thermal effects…
e.g.
Model reliability
(physically realistic, precision on refined parameters)
Long-range, perfectly ordered structure
Time-averaged “static” structure represents dynamics adequately
Crystal structure
(another model)
Measurable data
XRD
IR
Raman
Properties
Optical
Porosity
Guest affinity
Conduction

## Slide 7: Models are everywhere
Observation
Final model
Approximation, prediction
Model
Input
Output
Assumptions

## Slide 8: “All models are wrong, but some are useful”
https://en.wikipedia.org/wiki/All_models_are_wrong
G.E.P. Box, Journal of the American Statistical Association, Vol. 71, No. 356. (1976), pp. 791-799.
– George E. P. Box

## Slide 9: Crystallography
Modelling crystals

## Slide 10: XRD data to structural model
Model
Input
Output
Assumptions
Real crystal
Approximation of true atomistic arrangement (another model)
Ionic model
Hard spheres, known radii, electrostatic interactions
Crystalline solid
Regular repeat defined by periodic lattice

## Slide 11: XRD data to structural model
Model
Input
Output
Assumptions
Bragg’s law
Intensities
Structure factors
Thermal effects…
e.g.
Data reliability
(sample, measurement, processing…)
Long-range, perfectly ordered structure
Time-averaged “static” structure represents dynamics adequately
Crystal structure
(another model)

## Slide 12: XRD data to structural model
Model
Output
Bragg’s law
Intensities
Structure factors
Thermal effects…
Crystal structure
(another model)
Input
Positions Areas
Widths

## Slide 13: XRD data to structural model
Model
Input
Output
Assumptions
e.g.
Data reliability
(sample, measurement, processing…)
Background model
Diffraction peak shapes
Positions
Areas
Widths
Interpretation
more models!

## Slide 14: XRD data to structural model
Model
Output
Bragg’s law
Intensities
Structure factors
Thermal effects…
Crystal structure
(another model)
Input
Positions Areas
Widths
Using only Bragg peak information
Major assumption in crystallography
Perfect volume- and time-averaged model

## Slide 15: Modelling the diffraction pattern
Bragg’s law
Scattering intensities
reflection (hkl) positions
fj is the scattering factor for atom j at the position (xj,yj,zj) in the unit cell. For X-rays, it is related to the atomic number of j

## Slide 16: Analysis of diffraction intensities
…

## Slide 17
Inverse Fourier transform
(FT)-1
Fourier transform
FT
Real space: crystal structure
Reciprocal space: diffraction

## Slide 18: Structure determination from PXRD
Reliable intensities Ihkl from PXRD profiles can be challenging
  Reflections often overlap and cannot be fully resolved
If an approximate model of the crystal structure is available:
  Calculate diffraction pattern for the model
  Use least square refinement (minimisation) to vary the model parameters to produce a good match for the experimental data
Optimisation of a structural model to fit the whole experimental powder profile: Rietveld refinement

## Slide 19: Model refinement
Initial structural model
Unit cell and symmetry (crystal system, lattice centring, space group)
  a, b, c, a, b, g
  P, I, F
Atomic contents and positions
  For each atom: species (fj) position x, y, z atomic displacement b
Experimental model
Diffractometer
Data collection
↔︎ Positions of reflections︎
→ Systematic absences
→ Intensities
Sample model
Crystal size
Sample format
↔ Intensities
↔ Peak positions ↔ peak shapes

## Slide 20
where
Least squares
minimisation
S – goodness of fit F – structure factor
i – data points in profile K – hkl
w – weight s – scale factor
yo – observed intensity L – Lorentz polarisation factor
yc – calculated intensity – peak shape function yb – background intensity P – preferred orientation function
A – absorption (function)
Usual weighting scheme for PXRD:
s is standard uncertainty on the measured data point

## Slide 21: Bragg’s law
Parallel X-rays
wavelength l
Crystal planes
(hkl)
path difference
Remember: For constructive interference, PD = nl
For our purposes, n = 1
PD
For constructive interference, PD = nl

## Slide 22
experimental dataset calculated pattern difference reflection (hkl) position
Silicon crystal structure
Pat Woodward’s (OSU)
Rietveld refinement

## Slide 23: Accessing structural data
Crystal structures
  BYO – determined from diffraction
  ICSD
  CSD
  COD
  PDB, minerals, incommensurate
  Materials Project
  PCOD
  OQMD
Diffraction data
  ICDD (PDF-4/5+, etc.)
  P2D2 (from PCOD)
  BYO
  – collect data
  – from crystal structures
Notes: 105546

## Slide 24
https://github.com/rsc-solid-data/data_diffn_crystals

## Slide 25: Comparing XRD profiles
Be aware of where the cifs are from
  Experimental conditions
  Comparability of molecular simulations
Be aware of where the experimental data is from
  Experimental conditions
  Sample compositions (guest inclusion, compositional variation)
  Sample effects (size, preferred orientation, absorption, phase purity)
  Instrumental considerations (broadening, Lp, optics)
  Structural effects (order/disorder, symmetry, phase transitions)

## Slide 26: Comparing XRD profiles
Try the unit cell and space group
  Structureless refinement – no atoms, arbitrary intensities
  Le Bail or Pawley
Try a refinement
  Rietveld refinement is local minimisation
  Need a good starting model

## Slide 27: Some extra resources
Fundamentals of Powder Diffraction and Structural Characterization of Materials, Springer US, Boston, MA, 2009.
B. H. Toby, R factors in Rietveld analysis: How good is good enough?, Powder Diffr., 2006, 21, 67–70.
L. B. McCusker, R. B. Von Dreele, D. E. Cox, D. Louër and P. Scardi, Rietveld refinement guidelines, J Appl Cryst, 1999, 32, 36–50.
J. H. O’Donnell, R. B. Von Dreele, M. K. Y. Chan and B. H. Toby, A scripting interface for GSAS-II, J Appl Cryst, 2018, 51, 1244–1250.